## Slide 1: Unit-II
Equilibrium diagram and Iron -Iron Carbide Diagram

## Slide 2: Iron Iron Carbide Diagram

## Slide 3: Various phases that appear on the Iron-Carbon equilibrium phase diagram
Austenite
Ferrite
Pearlite
Cementite
Martensite*
Ledeburite

## Slide 4
d ferrite
BCC structure
Paramagnetic
a ferrite
BCC structure
Ferromagnetic
Fairly ductile

## Slide 5
g austenite
FCC structure
Non-magnetic
Ductile
Fe3C cementite
Orthorhombic
Hard
brittle

## Slide 6: Various Features of Fe-C diagram
Peritectic L + d = g
Eutectic L = g + Fe3C
Eutectoid g = a + Fe3C
Phases present
L
Reactions
d
BCC structure
Paramagnetic
g austenite
FCC structure
Non-magnetic
ductile
a ferrite
BCC structure
Ferromagnetic
Fairly ductile
Fe3C cementite
Orthorhombic
Hard
brittle
Max. solubility of C in ferrite=0.022%
Max. solubility of C in austenite=2.11%

## Slide 7: Phases in Fe–Fe3C Phase Diagram
a-ferrite - solid solution of C in BCC Fe
  Stable form of iron at room temperature.
  The maximum solubility of C is 0.022 wt%
  Transforms to FCC g-austenite at 912 C
g-austenite - solid solution of C in FCC Fe
  The maximum solubility of C is 2.14 wt %.
  Transforms to BCC d-ferrite at 1395 C
  Is not stable below the eutectic temperature (727  C) unless cooled rapidly (Chapter 10)
d-ferrite solid solution of C in BCC Fe
  The same structure as a-ferrite
  Stable only at high T, above 1394 C
  Melts at 1538 C
Fe3C (iron carbide or cementite)
  This intermetallic compound is metastable, it remains as a compound indefinitely at room T, but decomposes (very slowly, within several years) into a-Fe and C (graphite) at 650 - 700 C
Fe-C liquid solution

## Slide 8
C is an interstitial impurity in Fe. It forms a solid solution with a, g, d phases of iron
Maximum solubility in BCC a-ferrite is 0.022 wt% at727 C. BCC:relatively small interstitial positions
Maximum solubility in FCC austenite is 2.14 wt% at 1147 C - FCC has larger interstitial positions
Mechanical properties: Cementite (Fe3C is hard and brittle: strengthens steels. Mechanical properties also depend on microstructure: how ferrite and cementite are mixed.
Magnetic properties:  -ferrite is magnetic below 768 C, austenite is non-magnetic
Classification. Three types of ferrous alloys:
Pure Iron: < 0.008 wt % C in a-ferrite at room T
Steels: up to 2.14 wt % C (usually < 1 wt % ) a-ferrite + Fe3C at room T (Chapter 12)
Cast iron: 2.14 - 6.7 wt % (usually < 4.5 wt %)

## Slide 9: Invariant Reactions
Peritectic, at 1490 deg.C, with low wt% C alloys (almost no engineering importance).
Eutectoid, at 723 deg.C with eutectoid composition of 0.8wt% C, two-phase mixture (ferrite & cementite). They are steels.
Eutectic, at 1130 deg.C, with 4.3wt% C, alloys called cast irons.

## Slide 10
Peritectic L + d= g
Eutectic L = g + Fe3C
Eutectoid g = a + Fe3C
The diagram shows three horizontal lines which indicate isothermal reactions (on cooling / heating):
First horizontal line is at 1490°C, where peritectic reaction takes place:
Liquid +  ↔ austenite
Second horizontal line is at 1130°C, where eutectic reaction takes place:
liquid ↔ austenite + cementite
Third horizontal line is at 723°C, where eutectoid reaction takes place:
austenite ↔ pearlite (mixture of ferrite & cementite)

## Slide 11: Peritectic, at 1490 deg.C, with low wt% C alloys

## Slide 12
Eutectic and Eutectoid reactions in Fe–Fe3C
Eutectoid: 0.76 wt%C, 727 C
(0.76 wt% C)   (0.022 wt% C) + Fe3C
Eutectic: 4.30 wt% C, 1147 C
L   + Fe3C
Eutectic and Eutectoid reactions are important in heat treatment of steels

## Slide 13
Eutectic and Eutectoid reactions in Fe–Fe3C
Eutectoid: 0.76 wt%C, 727 C
(0.76 wt% C)   (0.022 wt% C) + Fe3C
Eutectic: 4.30 wt% C, 1147 C
L   + Fe3C
Eutectic and Eutectoid reactions are important in heat treatment of steels